-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep29lpaoht.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Thermally Conductive Epoxy for Large Potting Applications Features Low Exotherm

Master Bond EP29LPAOHT is a two component, NASA low outgassing approved epoxy system featuring a long working life of 8-10 hours per 1,000 gram batch. Due to its low exotherm and flowable consistency, this product is suitable for specialty potting applications where large masses of the epoxy need to be cured. It can be mixed and poured in volumes of more than a gallon at a time. Even in deep cross section thicknesses, this product does not generate much heat. Since the epoxy does not start gelling quickly, it is especially advantageous for use in many production environments that require a long open time after mixing.

EP29LPAOHT has a 100 to 50 mix ratio by weight and a mixed viscosity of 10,000-30,000 cps. It possesses a high thermal conductivity value of 0.87-1.15 W/(m•K), and is electrically insulative with a volume resistivity of more than 1015 ohm-cm. Upon curing EP29LPAOHT exhibits low shrinkage, dimensional stability and a low coefficient of thermal expansion. Other noteworthy properties include a compressive strength of 24,000-26,000 psi, a Shore D hardness of 80-90 and a tensile modulus of 450,000-500,000 psi. This epoxy is serviceable over the wide temperature range of -60°F to +350°F.

EP29LPAOHT bonds well to a variety of substrates including metals, glass, ceramics and many different plastics. It resists many chemicals including, but not limited to, water, fuels and oils. It is available for use in ½ pint, pint, quart and gallon container kits. EP29LPAOHT does not contain solvents and is RoHS compliant.

Master Bond Low Exotherm Epoxy Systems

Master Bond EP29LPAOHT is a NASA low outgassing certified two part epoxy featuring low exotherm along with high thermal conductivity and electrical insulation. This system also has a long open time and a moderate viscosity which is ideal for large potting applications. Read more about Master Bond’s low exotherm adhesives at https://www.masterbond.com/properties/low-exothermic-epoxy-systems or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep29lpaoht

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #