The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep35sp

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Epoxy Features Exceptional Chemical and Heat Resistance

Master Bond EP35SP is a two part epoxy system for bonding and sealing applications, providing resistance to many chemicals such as oils, acids, bases, water, fuels, and especially petrochemicals. It features both a high glass transition temperature (Tg) and a broad service temperature range. Its Tg measures 215-220°C and its serviceability extends from -62°C to +288°C (-80°F to 550°F).

EP35SP has notable dielectric properties with a dielectric constant of 4.5 at 60 Hz and a volume resistivity greater than 1014 ohm-cm. It bonds well to a wide array of substrates including metals, several plastics, ceramics, glass and composites. Upon curing, this system offers low shrinkage and good dimensional stability. Its tensile modulus is 550,000-600,000 psi with an overall superior physical strength profile even under adverse environmental conditions.

EP35SP has a paste viscosity, with little to no flow, and can be applied on vertical surfaces. The mix ratio is an easy to use 100 to 50 by weight. The system has a long working life of 24 to 48 hours. For optimal properties, the recommended cure schedule is 1 hour at 110°C followed by 2-3 hours at 125-150°C, plus a post cure at 175°C for 2-3 hours. Due to its high temperature resistance and structural properties, EP35SP may be considered for bonding and sealing in downhole, aerospace, electronic, optical and specialty OEM applications. Other uses may apply as well. The product is available in 1/2 pint, pint, quart, gallon and 5 gallon kits.

Master Bond High Tg Adhesives

Master Bond EP35SP is a two component epoxy system with high Tg and a paste consistency. It is formulated to withstand aggressive chemicals and high temperatures. Read more about Master Bond’s high Tg  adhesives at https://www.masterbond.com/properties/epoxy-adhesive-systems-high-glass-transition-temperature or contact technical support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/newsrelease/ep35sp

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #