-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep3htsda-2.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

One Part Silver Conductive Epoxy with Ultra High Heat Transfer Capability

Silver filled epoxy adhesive system Master Bond EP3HTSDA-2 was developed for crucial thermal management applications. As a one component system, it is not premixed and frozen and has an “unlimited” working life at room temperature. This compound possesses a high thermal conductivity of 45-49 BTU•in/ft2•hr•°F [6.5-7.0 W/(m•K)]. It can be applied in ultra thin bond lines and contains particles with an average size of 2-3 microns. Most importantly EP3HTSDA-2 exhibits very low thermal resistance of 2-3 x 10 -6 K•m2/W. It also has outstanding electrical conductivity with a volume resistivity less than 0.001 ohm-cm.

EP3HTSDA-2 meets NASA low outgassing specifications and is serviceable from -80°F to +450°F [-62°C to +232°C]. This product adheres well to similar/dissimilar substrates such as aluminum, ceramic, copper, fiberglass, polyimide and silicone die. This formulation is designed to cure in 20-30 minutes at 250°F or 5-10 minutes at 300°F. Die shear strength has a 20-20 Kg-f value at 75°F measured for a die size of 2x2 mm [80x80 mil].

EP3HTSDA-2 is packaged in syringes or glass jars. Common sizes range from 20 grams, 50 grams, 100 grams to one and multiple pound units. For storage simple refrigeration is recommended. Shelf life is a minimum of 3 months in original unopened syringes or jars.

Master Bond Thermally Conductive Adhesives

Master Bond EP3HTSDA-2 is a single component, heat curable, thermally and electrically conductive epoxy. It is NASA low outgassing approved and offers thermal stability along with high strength properties. Read more about Master Bond’s thermally conductive adhesives at https://www.masterbond.com/properties/thermally-conductive-epoxy-adhesives  or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep30htsda-2

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #