The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep42ht-3ao .

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Thermally Conductive Potting Compound Features a Low Coefficient of Thermal Expansion

Master Bond EP42HT-3AO is a two component, moderate viscosity epoxy system with good flow properties. It is ideal for small to moderate size encapsulating, potting and casting applications. It is also effective in bonding fragile components requiring a low coefficient of thermal expansion. EP42HT-3AO is designed to optimize heat dissipation properties, improve the quality and reliability of electronic devices subjected to thermo-mechanical stresses.

This compound combines a low CTE of 13-16x 10-6 in/in/°C with a high glass transition temperature (Tg) of 140-150°C. It has a thermal conductivity of 11-12 BTU•in/ft²•hr•°F [1.59-1.73 W/(m•K)]. It also exhibits low shrinkage upon curing, dimensional stability, and excellent structural strength. EP42HT-3AO is a reliable electrical insulator with a volume resistivity of >1014 ohm-cm. This system is serviceable from -100°F to +400°F.

This 100% reactive epoxy formulation has a non-critical 100 to 40 mix ratio by weight and a working life of 60-90 minutes after mixing for a 100 gram batch at 75°F.  It has a recommended cure schedule of overnight at room temperature, followed by 2-3 hours at 150-200°F. EP42HT-3AO is available for use in ounce, ½ pint, pint, quart and gallon kit containers. Specialty packaging options in the form of pre-mixed and frozen syringes are also available. The specialty packaging allows for automated dispensing. The color of Part A is white and Part B is off-white.

Master Bond Epoxies for Potting Applications

Master Bond EP42HT-3AO is a two component epoxy system for bonding, potting and encapsulation applications, featuring a low coefficient of thermal expansion, high Tg, excellent chemical resistance and reliable electrical insulation properties. Read more about our formulations for potting applications at https://www.masterbond.com/applications/potting-and-encapsulation  or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep42ht-3ao

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #