---------------------------------------------------------------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep64.

---------------------------------------------------------------------------------------------------------------------

FOR IMMEDIATE RELEASE

NASA Low Outgassing, Chemically Resistant Epoxy Features High Tg

Master Bond EP64 is a two-component, vacuum-compatible epoxy system engineered for bonding, sealing, and coating applications. It features a high glass transition temperature (Tg) of 210–215°C and meets NASA low outgassing specifications per ASTM E595 testing. This product is resistant to a variety of chemicals—including acids, bases, and many solvents—and serves as a dependable electrical insulator.

EP64 has a tensile strength of 3,000–5,000 psi and a tensile modulus ranging from 540,000–680,000 psi at room temperature. The system exhibits a Shore D hardness of 80–90. It is serviceable over a temperature range of -60°F to +450°F (-51°C to +232°C), making it suitable for aerospace and electronic applications requiring stable performance under vacuum conditions.

This system features a working life of 12–24 hours for a 100-gram batch at room temperature and has a moderate viscosity with good flow properties. The recommended cure schedule is 80–90°C for 4–6 hours, followed by a post cure at 120–130°C for 2–4 hours to reach its full performance profile. Achieving a Tg of 210–215°C with such a cure profile is the key distinguishing characteristic of this system. EP64 bonds to substrates including metals, plastics, rubbers, ceramics, and composites. It is available in standard packaging ranging from 1/2 pint to gallon kits, as well as in premixed and frozen syringes.

Master Bond High Glass Transition Temperature Adhesives

Master Bond offers a selection of high Tg epoxy and UV-curable systems. These materials maintain mechanical strength, thermal stability, and electrical insulation properties at elevated temperatures more effectively than systems with a lower Tg. To learn more about high glass transition temperature systems, visit https://www.masterbond.com/properties/epoxy-adhesive-systems-high-glass-transition-temperature or contact our technical support team to discuss your specific application requirements.

TECH SUPPORT

Email: technical@masterbond.com

Web: https://www.masterbond.com/contact

Tel: +1-201-343-8983

Note to Editors:

For a full product description, please visit https://www.masterbond.com/tds/ep64.

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com