-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep88fl

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Optically Clear, Low Viscosity Epoxy System Features High Flexibility

Two component epoxy, Master Bond EP88FL, is a highly flexible, optically clear compound formulated for bonding, coating, sealing, potting and encapsulation. It is easy to use, with a mixing ratio of one to one by weight or volume.

EP88FL withstands thermal cycling and shock. It is ideal in applications where stress relief is needed with a tensile modulus ranging from 10,000 psi to 20,000 psi. This system provides an elongation of 30-50% and bonds well to a wide variety of substrates such as metals, ceramics, plastics and glass. Despite curing with a good degree of flexibility, it cannot be considered soft since it has a Shore D hardness between 45-55 at 75°F. The refractive index is 1.51 at 589 nm, making the system relevant for applications in optics, opto-electronics, aerospace and OEM.

The mixed viscosity of EP88FL is 800-1,200 cps at room temperature, and its working life is 20-30 minutes for a 100 gram batch.  EP88FL can be cured at room temperature or elevated temperatures. The optimal cure is overnight at 75°F plus 1 to 2 hours at 150-200°F. Master Bond EP88FL is available in standard packaging ranging from ½ pint to 5 gallon containers as well as specialty packaging including FlexiPaks®, syringes and gun dispensers.

Master Bond Optically Clear Epoxy Systems

EP88FL is a free-flowing, highly flexible, stress absorbing epoxy with a low modulus of elasticity. It is optically clear with a refractive index of 1.51. Read more about Master Bond’s optically clear adhesive systems at https://www.masterbond.com/properties/optically-clear-polymer-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep88fl

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #