The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/mastersil-170-gel .

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Extremely Soft MasterSil 170 Gel Encapsulant Offers Removability and Optical Clarity

Master Bond MasterSil 170 Gel is a two component system with excellent flowability for potting and encapsulation applications. It possesses a low mixed viscosity of 1,000 cps, has a long working life after mixing (2-4 hours for 100 g batch), a low exotherm upon cure and is easy to dispense. This solvent free silicone product does not require exposure to air for cross-linking. It has a convenient one to one mix ratio by weight and will cure at 75°F or more quickly at elevated temperatures.

“MasterSil 170 Gel has excellent optical clarity” says Rohit Ramnath, Senior Product Engineer. “It has a low refractive index of 1.42. Additionally, it exhibits outstanding electrical insulation properties, can cure in thicknesses beyond 1 inch, protects sensitive electronic/optical components against thermal stresses. Most notable for MasterSil 170 Gel is the ability it offers to retrieve delicate components after cure.”

This versatile composition is highly resistant to water, is able to withstand severe thermal cycling without cracking and has extremely low shrinkage upon cure. This soft, pliable and compliant silicone system is repairable and its hardness penetration is 65 mm. MasterSil 170 Gel is available for use in ½ pint, pint, quart, gallon and 5 gallon kit containers. Shelf life in original, unopened containers at 75°F is 6 months.

Master Bond Optically Clear Adhesives

Master Bond 170 Gel is a high temperature resistant, two component silicone gel that features electrical insulation properties, resistance to vibration, thermal cycling. This low stress system also features optical clarity and removability. Read more about our optically clear adhesives at https://www.masterbond.com/properties/optically-clear-polymer-adhesives  or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/mastersil-170-gel

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #