-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/mastersil-981-lo.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Optically Clear, High Flexibility Silicone Meets NASA Low Outgassing Specifications

Master Bond MasterSil 981-LO is a two component, addition cured silicone system designed for bonding, sealing, coating, and encapsulating applications. It meets NASA low outgassing specifications and features optical clarity, particularly in thin sections, making it well suited for aerospace, satellite, optical, and optoelectronic applications. The compound is 100% reactive, contains no solvents or diluents, and exhibits minimal shrinkage upon cure.

MasterSil 981-LO features a Shore A hardness of 20–30, a low modulus, and good flexibility, with an elongation of 200–300% at 75°F. It withstands thermal shock and cycling without cracking or imparting stress on bonded components. The system is serviceable over a temperature range of -65°F to +400°F (-54°C to +204°C) and provides electrical insulation properties, including a dielectric strength of 450 volts/mil (1/8 inch thick specimen) and a volume resistivity greater than 10¹⁴ ohm-cm at 75°F. The refractive index measures 1.437.

This system features a forgiving 1:1 mix ratio by weight and a flowable, mixed viscosity of 12,500–17,500 cps at room temperature. Its 3–4 hour working life for a 100-gram batch allows sufficient time for application and processing. The recommended optimal cure schedule is overnight at room temperature, followed by 2–4 hours at 135°F to 165°F. MasterSil 981-LO bonds to a variety of substrates, including metals, glass, plastics, ceramics, and many silicone rubbers. It is available in standard packaging ranging from 30 cc syringe kits to gallon kits, and is compatible with gun dispensers for automated applications.

Master Bond Low Outgassing Adhesives

Master Bond offers an extensive portfolio of low outgassing adhesive systems formulated for applications where vacuum compatibility and reliability are essential. These chemistries include epoxies, silicones, UV curables, and specialty compounds designed for use in aerospace, satellite, optical, and electronic environments. Select grades meeting NASA low outgassing specifications provide performance properties such as strong adhesion, electrical insulation, thermal stability, optical clarity, flexibility, and resistance to thermal shock. To learn more about low outgassing systems, visit https://www.masterbond.com/properties/low-outgassing-adhesives or contact technical support to discuss your application.

TECH SUPPORT

Email: technical@masterbond.com

Web: https://www.masterbond.com/contact

Tel: +1-201-343-8983

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/mastersil-981-lo

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #