-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/supreme-10htlv.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Structural One Part Epoxy for High-Performance Bonding Applications

Master Bond Supreme 10HTLV is a one part, non-frozen, heat cured epoxy formulated for demanding structural bonding applications. This toughened system features a moderately high viscosity with good flow, which will not thicken over time. It is ideal for applications requiring strong, durable bonds, replacing traditional mechanical fastening. With an unlimited working life at room temperature, Supreme 10HTLV offers convenient storage, simplified handling and streamlined processing.

Supreme 10HTLV is engineered for extreme environments, withstanding cryogenic temperatures down to 4 K and serviceable at temperatures as high as 400°F. It ensures long term reliability under dynamic conditions by enduring mechanical shock, vibration, and severe thermal cycling. The system demonstrates excellent environmental resistance, surviving 1,000 hours at 85°C/85% RH and exhibiting strong protection against water, oils, and various chemicals. Delivering high mechanical performance, this epoxy achieves tensile shear strengths over 3,600 psi and T-peel strengths up to 30 pli. Supreme 10HTLV is electrically insulative, providing a volume resistivity greater than 10¹² ohm-cm at room temperature, and bonds well to metals, glass, ceramics, and many plastics.

Its versatile heat-curing profile offers two convenient options: 60–75 minutes at 250°F or 35–40 minutes at 300°F. No mixing is required. Supreme 10HTLV is standardly available in gray, with additional colors available upon request. It is packaged in ½-pints, pints, quarts, gallons, and specialty containers, including cartridges and syringes, to accommodate diverse production needs.

Master Bond Epoxy Systems that Pass 85°C, 85% Relative Humidity Testing

Master Bond offers an extensive range of high-performance compounds—including one and two part epoxies, silicones, and LED/UV curable systems—that have successfully passed Telcordia GR-1221 test specifications for damp heat storage. These materials are used in optical, electronic, and optoelectronic applications where device reliability is critical. For more information on this rigorous testing and the certified Master Bond adhesives, please visit the certification page at https://www.masterbond.com/certifications/85c-85humidity-testing or contact technical support to discuss your application.

TECH SUPPORT

Email: technical@masterbond.com

Web: https://www.masterbond.com/contact

Tel: +1-201-343-8983

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/supreme-10htlv

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #