Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.  This email was sent to (%email%)

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/newsrelease/led401.

----------------------------------

FOR IMMEDIATE RELEASE

One Component LED Curable System Offers Exceptionally Fast Cure Speeds

Cures Completely Tack-Free Without Requiring UV Light

HACKENSACK, NJ – October 18, 2012 – Master Bond LED401 is a breakthrough system based on LED technology. This adhesive, sealant, coating and encapsulant cures tack-free upon exposure to a 405 nm wavelength light source, without any oxygen inhibition. Optically clear, it is also safer and easier to handle than similar UV systems as LED lights emit substantially less heat than UV lamps. This makes LED401 a suitable choice for applications involving heat sensitive substrates.

As a one part system, LED401’s open time is indefinite. It is a higher viscosity system at 100,000-150,000 cps, but maintains its flowability and convenient handling. With cure times of 15 to 30 seconds or less in thinner sections, depending upon the distance of the light source from the material being cured, it can also be readily cured in sections up to 1/8 inch thick. It bonds well to similar and dissimilar substrates, including most plastics, metals and ceramics. Additionally, this compound has superior adhesion to glass, polycarbonates and acrylics.

LED401 offers excellent resistance to a variety of chemicals including water, many acids, bases and oils. It has superior electrical insulation properties with a volume resistivity exceeding 1014 ohm-cm. Serviceable over the wide temperature range of -60°F to +250°F, LED401 features very good dimensional stability.

Master Bond LED401 has a shelf life of six months at room temperature without exposure to light, in its original containers. It is available in syringes, ½ pints, pints, quarts, gallons and 5 gallon containers. Other versions of this product are available with different viscosities and in an opaque white color.

Master Bond Optically Clear Adhesives

Formulated for high performance bonding, sealing, coating and encapsulation applications, optically clear LED401 offers excellent light transmission and rapid LED cures. Read more about Master Bond’s optically clear adhesives at http://www.masterbond.com/properties/optically-clear-polymer-adhesives or contact Technical Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

# CONTACT:

# James Brenner, Marketing Manager

# Email: jbrenner@masterbond.com

# Tel: +1-201-343-8983

Fax: +1-201-343-2132

# MASTER BOND INC.

# 154 Hobart Street

Hackensack, NJ 07601-3922

# Web: www.masterbond.com

# # #